https://pubs.rsc.org/en/content/articlelanding/2017/cs/c6cs00066e#!divAbstract

M-47

#23
@@@
 7. Conclusions and outlook

The conversion of CO2 – preferably into value-added products – is considered one of the great challenges of our century.

 In the past decade,

 substantial progress with several novel technologies has been made.

 The last section of this review intended to provide the reader with a state-of-the art and critical assessment of an – up till now – rather underexposed emerging technology: the plasmachemical conversion of CO2. To achieve this,

 we provided an introduction to the basic concepts of plasma,

 and we demonstrated its viability as a gas conversion technology,

 finally putting it in the broader context of its peers.

From the advances in the area of CO2 conversion discussed in this review,

 one outcome stands out without doubt.

 The question is not ‘if’ one of these novel technologies will be industrially competitive,

 but rather ‘when’ and ‘which one(s) will play the leading role’.

 To shine a brighter light on – the final burning question – whether plasma technology could be the answer – or at least be part of the equation – we briefly summarize here the arising opportunities and challenges for plasma technology in the field of CO2 conversion.

#23.1
Plasmas possess some important advantages over certain other (novel) technologies: (i) they can operate at room temperature using any source of (renewable) electricity,

 (ii) they have a large flexibility in terms of the feeds that need to be processed,

 (iii) they provide an extremely flexible ‘turnkey’ process,

 which allows for the efficient storage of energy,

 peak shaving and grid stabilization,

 (iv) the reactors have low investment and operating costs,

 (v) they have a simple scalability both in size and applicability,

 and (vi) last but not least,

 the technology does not rely on rare earth materials – making it rather unique at this point.

 This unprecedented combination of features gives plasmachemical conversion a very high overall flexibility,

 making it an extremely useful and valuable technology for CCU.

The flip side of the coin is that the reliance of plasma technology on indirect solar energy in the form of electricity is – at the same time – a limiting factor for the solar-to-fuel conversion efficiency,

 especially compared to technologies that can directly harvest solar energy.

#23.2
 Nonetheless,

 this also allows plasma technology to rely on other renewable energy sources,

 and more importantly,

 it adds to its overall – location and process – flexibility,

 since it is not dependent on the availability of sunlight.

 More urgent,

 however,

 is the issue of product separation.

 From all the data available in the literature,

 it is clear that converting CO2 – with or without an additional hydrogen source – always yields a mixture of products after reaction.

 This implies the need for an – often expensive – post-processing separation step.

#23.3
From the benchmarking discussion,

 it is clear that plasma technology can definitely play an important role in the field of CO2 conversion,

 and it is not beyond our grasp to think about its eventual commercial implementation,

 be it on a large or small scale.

 Nevertheless,

 as always,

 only a few candidates seem suitable for the specific task at hand,

 as we outline here.

#23.3.1
Two main CO2 conversion strategies were discussed: (i) pure CO2 splitting and (ii) CO2 conversion in combination with a co-reactant serving as the hydrogen source,

 i.

e. CH4, H2 and H2O, yielding processes named the dry reforming of methane (DRM),

 the hydrogenation of CO2 and artificial photosynthesis,

 respectively.

#23.3.2

 At this time,

 the conversion of CO2 through the latter two processes is – although possible – inefficient in a plasma-only set-up,

 not to mention industrially undesirable,

 due to the formation of possibly dangerous mixtures to be handled.

#23.3.3
 In the future,

 the combination of plasma with other technologies,

 such as catalysis or electrolysis,

 could solve these issues.

 On the contrary,

 for both pure CO2 splitting and DRM,

 the proposed energy efficiency target of 60% has already been surpassed by several types of plasma reactors,

 resulting in a solar-to-fuel conversion efficiency for the production of syngas above – the required – 20% mark.

#23.3.4
In the short run,

 pure CO2 splitting using the most energy-efficient set-ups,

 i.

e. MW and GA discharges,

 appears to have a high potential.

 In this case,

 pure CO and O2 could be produced,

 after a separation step,

 or a pure CO stream when in situ trapping of the O2 can be successfully implemented,

 e.

g. by combination with other technologies or through the addition of scavengers.

#23.3.5

In the long run,

 it seems evident that CO2 conversion in combination with a hydrogen containing co-reactant has the highest potential for the efficient production of value-added products,

 such as alcohols,

 aldehydes,

 esters and acids.

 In particular,

 the %%direct oxidative pathway[직접 산화 경로,

 in which the intermediate syngas step is circumvented,

 has great potential.

#23.3.6
 For now,

 however,

 a lot of research in this area is still needed to #%increase the selectivity towards these valuable bulk chemicals over the currently produced syngas.

 This will most probably need to be achieved in combination with catalysts.

 However,

 even today,

 APGD and GA discharges already provide an energy-efficient alternative to produce syngas in any desired ratio through DRM.

#23.3.7

By all means,

 plasma technology is not just an overlooked unicorn – although its combination of features does make it quite unique for CCU – but,

 as mentioned several times throughout this work,

 and just like for all other emerging technologies in this field,

 several important challenges remain.

#23.4
 General challenges comprise the need for further fundamental research,

 concerning: (i) the plasmachemical processes taking place in warm discharges,

 such as MW and GA,

 which stimulate vibrational excitation; whereby the latter,

 representing the most energy-efficient dissociation pathway,

 should be further exploited by enhancing the non-equilibrium character of these plasmas to further improve the energy efficiency,

 (ii) the combination of plasma with catalysis and the possibility of taking advantage of the synergetic effects and the selective production of value-added compounds,

 (iii) in situ O/O2 trapping by using scavengers,

 or combinations with other technologies,

 such as catalysis or %%SOEC,

 to further enhance the conversions and yields towards the desired value-added compounds,

#23.4.1
 (iv) the demonstration of successful scale-up for other discharges than DBDs and (v) the production and tuning of efficient power supplies for generating and sustaining the plasma.

#23.5
Moreover,

 some important discharge-specific research challenges can also be identified.

 For MW plasmas,

 the ultimate goal should be to achieve the same energy efficiency at atmospheric pressure as currently obtained at reduced pressure for CO2 splitting,

 while more research towards DRM is essential.

 For GA plasmas,

 the limited amount of gas that passes through the active arc region,

 and thus that can be converted by the plasma,

 is currently limiting the overall CO2 conversion,

 and more research in this direction is needed,

 e.

g. by improving the reactor design.

#23.5.1
 Furthermore,

 some other plasma reactors show good performance,

 but the available data and insights are still limited,

 thus requiring more research to explore their full potential.

#23.5.2
 Of course,

 inherent to every review,

 the above analysis represents the current state-of-the-art.

 Plasma-technology-based CO2 conversion is relatively new and it is clearly a fast advancing field with – just like for any emerging technology – ample room for improvement and new (interdisciplinary) developments.

#23.5.3
It appears that the ultimate plasma for CO2 conversion would be a system with a high electron density (Ne) and a low electron temperature (Te) – resulting from a low reduced electric field (E/n) – which are essential to stimulate and achieve a high fraction of vibrational excitation.

 At the same time,

 this system should operate at a low gas temperature (Tg) to minimize the VT relaxation losses and backward recombination reactions.

#23.6
 Finally,

 to be industrially attractive,

 this should be achieved at atmospheric pressure.

Future research towards the #%direct oxidative production of oxygenates,

 as well as multi-reforming processes with a combination of gases (e.

g. CO2, CH4 and H2O or O2) or several reforming processes in series,

 using plasma technology appears very promising and should be pursued.

#23.6.1

 Furthermore,

 more interdisciplinary research into the combination of plasmas with other novel technologies is highly desirable.

#23.6.2

 For catalysis,

 the combination is already proving alluring,

 and it is our opinion that %#combinations with electrolysis,

 although even more challenging,

 could also lead to synergetic effects.

 As is the case for many important issues brought forward in the current age,

 with a high probability the future will rely on a true amalgam of technologies and solutions,

 each for its specific tasks,

 rather than the ‘one solution (or technology) fits all’ mentality of the old age.

#23.7

From the current analysis,

 it is evident that pure CO2 splitting could reach industrial implementation at a faster pace.

#23.7.1
 Nevertheless,

 CO2 conversion using a hydrogen source as a co-reactant should certainly be further pursued,

 since – when successful – in the long run it offers us the possibility of %#producing a wide variety of value-added chemicals and fuels,

 starting from the same building block and allowing the flexibility to tune the output depending on the market's needs.

 On that account,

 we believe plasmas could be – at least part of – the bright light that shines on our horizon.

Acknowledgements

We would like to thank W.

 Wang (University of Antwerp) for providing the data on the thermal equilibrium conversions.

 Furthermore,

 we acknowledge financial support from the IAP/7 (Inter-university Attraction Pole) programme ‘PSI-Physical Chemistry of Plasma-Surface Interactions’ by the Belgian Federal Office for Science Policy (BELSPO),

 the Methusalem financing of the University of Antwerp,

 the Fund for Scientific Research Flanders (FWO; Grant no.

 G.

0383.16N, G.

0254.14N and G.

0217.14N),

 the TOP research project of the Research Fund of the University of Antwerp (grant ID.

 32249).

#24
 4.3. Plasma-catalysis

As with most of the technologies described in Section 3, plasma set-ups can also be combined with a packing material or catalyst,

 giving rise to plasma-catalysis.

 Plasma-catalysis is an emerging branch of plasma processing at the interface of a variety of disciplines,

 including physical chemistry,

 material science,

 nanotechnology,

 catalysis,

 plasma physics and plasma chemistry.

 In short,

 its objective is to enhance plasma reactions by adding a catalyst to the reaction cycle and vice versa.

#24.1
 Theoretically speaking,

 combining plasma with catalysis offers the best of both worlds.

 Inert molecules are activated by the plasma under mild conditions,

 and subsequently the activated species selectively recombine at the catalyst surface to yield the desired products.

 This will be especially important to further advance and optimize the %%direct oxidative liquefaction pathway of plasmachemical CO2 conversion,

 in order to selectively produce the desired liquid products.

#24.2
 In this section,

 we present a brief overview of the different approaches and possible interactions between the plasma and the catalyst.

 For more extensive details,

 we refer to several broad reviews on this specific topic that have recently been published.

83,102–104
4.3.1. Approaches

Plasmas and catalysts can be combined in two main configurations,

 as illustrated in Fig.

 16. In the first,

 the so-called two-stage configuration (Fig.

 16(b)),

 the catalyst is spatially separated from the plasma region,

 either upstream or downstream,

 but the main configuration is downstream.

 In the second,

 the so-called one-stage configuration (Fig.

 16(c)),

 the catalyst is placed inside the discharge region.

 In a traditional thermal catalysis experiment,

 molecules are dissociatively adsorbed onto the catalyst with the energy being supplied in the form of heat.

 In plasma-assisted catalysis,

 species are activated by the plasma due to excitation,

 ionization or dissociation by electrons in the gas phase or on the catalyst surface.

 The major difference between the one-stage and two-stage configuration is the kind of species to which the catalyst is exposed.

 In the two-stage configuration,

 the end-products and the long-lived intermediates will interact with the catalyst,

 while in the one-stage configuration,

 the catalyst can also interact with all the short-lived species,

 including excited species,

 radicals,

 photons and electrons.

 Furthermore,

 in this configuration the catalyst may also be influenced by the plasma and vice versa (see below).

#24.3
 Besides plasma-catalysis,

 the #%preparation and modification of catalysts by plasma treatment is gaining increased attention,

 especially for catalysts with a low thermal stability.

103

The most widely investigated and,

 for this review,

 most interesting configuration is the one-stage configuration,

 in which the catalyst is placed inside the discharge region,

 either completely or only partially occupying the discharge zone.

 The catalyst itself can be introduced in the discharge as pellets,

 (fine) powders,

 foams,

 %%honeycomb monoliths,

 different electrode materials and electrode coatings or as coated %%quartz wool.

 The ease of adding a catalyst into the discharge zone greatly varies depending on the type of plasma reactor used.

#24.4
 In general,

 due to their simple geometry and operation close to room temperature,

 implementation of a catalyst in a DBD reactor is very easy.

 Although MWs also have a simple geometry,

 due to the high gas temperature inside the discharge zone (1000–2000 K compared to 300–400 K for DBD) catalysts are often placed downstream,

 due to their low thermal stability.

 Finally,

 GA discharges have rather complex geometries and the same higher gas temperatures,

 thus catalysts are typically introduced downstream,

 although the use of a %%spouted bed has also been reported.

105 If these MW and GA discharges can be operated at slightly lower temperatures (≤1000 K),

 this would yield new possibilities.

 It would also open up the way for using sufficiently thermally stable catalysts inside the discharge zone,

 and at the same time it would allow thermal activation of catalysts inside the discharge zone by the plasma.

#24.5
4.3.2. Synergetic effects

The resulting interactions when combining a plasma with a catalyst for plasma-based CO2 conversion often yield improved process results in terms of conversion,

 selectivity,

 yield and energy efficiency.

 This surplus effect,

 as shown in Fig.

 17, is a complex phenomenon originating from the interplay between the various plasma–catalyst interactions and is often termed ‘synergy’,

 when the combined effect is larger than the sum of the two separate effects.

102 Note that most research to date regarding this effect #%has been performed for DBDs.

 The complex interactions can be subdivided into two categories: the effects of the plasma on the catalyst,

 and vice versa,

 the effects of the catalyst on the plasma.

102,107 Second,

 it is important to distinguish between the two types of effects: physical and chemical effects.

 While the physical effects are mainly responsible for gaining a better energy efficiency,

 the chemical effects can lead to an improved selectivity towards the targeted products.

 In the case of CO2 splitting,

 mainly CO and O2 are formed,

 so the primary added value of the catalyst is to increase the energy efficiency,

 although the conversion can also be improved by chemical effects,

 such as enhanced dissociative chemisorption due to the catalyst acid/basic sites.

 When adding a co-reactant (e.

g. CH4, H2O, H2), the catalyst allows modifying the selectivity towards the targeted products.

#24.6

An overview of the plasma–catalyst interactions is given in Fig.

 18. When adding a catalyst,

 the following effects on the plasma have been reported: (i) an enhancement of the electric field through the geometric distortion and surface roughness; (ii) the formation of micro-discharges inside the pores of the catalyst material,

 due to the very strong electric field inside the pores,

 leading to different characteristics compared to the bulk; (iii) a change in the discharge type,

 because the presence of insulating surfaces promotes the development of surface discharges; (iv) the adsorption of species on the catalyst surface,

 which affects their concentration and conversion due to longer retention times.

 All the effects of the catalyst on the plasma can thus generally be considered as physical effects.

 The reported effects of the plasma on the catalyst,

 on the other hand,

 are of both a physical and chemical nature.

 They include: (i) changes in its physico-chemical properties,

 such as a higher adsorption probability at the catalyst surface,

 a higher catalyst surface area,

 a changed catalyst oxidation state,

 the reduction of metal oxide catalysts to their metallic form,

 reduced coke formation on the surface and a change in the catalyst work function; (ii) the formation of hot spots on the surface due to the formation of strong micro-discharges; (iii) catalyst activation by photon irradiation emitted by the excited plasma species (although this effect is probably of only minor importance due to the low photon fluxes); (iv) lowered activation barriers due to there being more reactive vibrationally excited plasma species and consequently a greater possibility for non-adiabatic barrier crossings; (v) changes in the reaction pathways due to the presence of a wide variety of (re)active species.

#24.7
While the physical effects have been more extensively studied,

 such as the plasma behaviour in packed-bed DBD reactors108 or inside catalyst pores,

109 the chemical effects are less understood,

 mainly because they are often correlated with the physical effects.

 Indeed,

 in a DBD,

 the catalyst is mostly introduced as a packed bed,

 making it difficult to distinguish between the two effects.

 Hence,

 more systematic studies on both the physical and chemical effects of the catalyst material are highly needed.

102 Furthermore,

 as summarized in Fig.

 19, the plasma and catalyst both have an influence on the gas composition,

 and at the same time the plasma influences the catalyst properties and vice versa,

 as mentioned above.

 Therefore,

 both the gas composition and the plasma and catalyst properties continuously influence each other,

 and at the same time are influenced by the plasma chemistry and surface chemistry.

 Thus,

 it is recommended to develop tailored catalysts for plasma-catalysis,

 rather than simply relying on classical catalysts.

 This is discussed further in Section 5.

Finally,

 it is worth mentioning that besides CO2 conversion,

 the combination of plasma with catalysts is also promising for nanomaterial synthesis,

 such as for the growth of carbon nanotubes,

 nanofibres,

 and graphene.

 To date,

 research on this topic has been mainly focused on pure methane plasmas,

 instead of CO2 plasmas.

 This is,

 however,

 outside the scope of the present review,

 but we refer to another recent review paper,

 where these applications are discussed in detail.

102

]XXX

------------------------------------------ [resource] 20200526_153656
#%Plasma-Driven Catalysis	keyword	青２
%%flexibility to be scaled up and down	notice	緑４
#2	location number	青２ / オレンジ色１

1	([^\d])(\.|\,)	$1$2\n\n
	([^\d]{2,}?)(\.|\,)	$1$2\n\n

/ ------------------------------------------ [resource] 20200526_153656 /